SOLTECH technical bulletin (silk screen ink)

Guide formulation of silk screen ink

% by wt.

Pigment + filler				10 – 30

Acrylate resin(Oligomer)			35 – 60

Diluents(monomer)			15 – 50

Photo-initiator				 3 -  7

Additive(adhesion, leveling, reology)  	 1 -  5

Oligomer

Solmer E-1702 : standard resin for screen ink.

Fatty acid modified epoxy acrylate.

Excellent flow and pigment wetting.

High gloss and solvent resistance.

Solmer E-1703: : standard resin for screen ink.

Amine modified epoxy acrylate with fatty acid.

Excellent cure speed and pigment wetting.

High gloss and good adhesion.

Solmer P-2250: polyester acrylate with TPGDA

Excellent adhesion on glass and plastic.

Solmer P-236: polyester acrylate with TMPTA

Excellent adhesion on plastic and metal.

Good pigment wetting.

Solmer U-584: non-yellowing urethane acrylate.

Good adhesion on various substrates.

Excellent flexibility.

Solmer A-345: acrylic acrylate with monomer.

Use additive as adhesion promoter.

Excellent intercoat adhesion.

High flexibility.

Solmer U-88: aromatic urethane hexa-acrylate.

Use additive to improve curing speed.

# We recommend to use oligomers combine more than two types for final performance.

Monomer

TMPEOTA : good litho-property.

HDDA : excellent viscosity reduction.

TPGDA : reasonable price and low viscosity.

Photo-initiator

Chivacure TPO, 107, 173, BMS, OMB, EMK, ITX, BP, EPD.

# Refer to UV absorbance band.

Additive

Solmer Z-9166 : methacrylic acid type adhesion promoter.

Solmer Z-9167 : acrylic acid type adhesion promoter.

Solmer Z-9070 : non-silicone leveling agent.